## Slide 1: Introduction to dataset collection
GitHub KEM292

## Slide 2: Aim
Build a video and image dataset to train a code on discerning and recognizing visual cues during digestion of a gelatin gel.

## Slide 3: Gel casting
Gel casted is a 3% w/V gelatin gel in ultra-pure water, crosslinked with TGM to make it resistant to body temperature (37⁰C) and with a yellow food dye to make it colored.
The video recordings for the dataset were collected using the microscope probe in the pictures on the left (https://www.amazon.se/Staright-Microscope-Inspection-Magnification-Smartphones/dp/B09FZ541PT?source=ps-sl-shoppingads-lpcontext&ref_=fplfs&psc=1&smid=A3D3WC8ILPB8DS)
Microscope probe
Neutral booth where we recorded the videos with the closed box

## Slide 4: Gel Casting Conditions
Gelatin swelling
3 % m/V
30 min
10 min
40 min
10 min
Gel casting
Warming gelatin
45°C
TGase deactivation
80°C
TGase crosslinking
45°C
65 µl TGase is added
100 µl yellow food colouring
Notes: Gelatin Type A (Bloom 300 g, porcine skin, Sigma-Aldrich)
TGase (Galaya® Prime, Novozyme)
yellow food colouring (Dr.Oetker)

## Slide 5: Gel casting The gel was casted in slightly different ways on the microscope probe
With a straw
Using a plastic straw to deposit 0.8 cm-think gel in front of the microscope camera
Without a straw
Just depositing 0.2 cm-thick gel in the concavity in front of the microscope camera
Named “…_without_straw_...”
Used in the “new setup” and with a better outcome
Named “…_with_straw_...”
Used mostly in the old setup during July and August, but no more in the new setup

## Slide 6: Setups - Put in a water bath with different media conditions (pH, IS, presence of pepsin). - The neutral booth setup was employed to avoid any lighting difference coming from the room. - Connect the camera to a computer with OBS (Open Broadcaster Software). - Recorded it for 10 hours.
July folder
A trial period to get to chose the best setup. Some video has the probe completely enveloped in gel, some other with a straw but a layer of air in between the camera and the gel.
Check it out, but it is worth to check the rest more
With a straw
Especially in August the straw setup (check previous slide) has been employed, but it was missing a white paper below the water bath (to avoid reflection from the heating plate) and OBS was set to autoexposure, which automatically changed the exposure value in the recorded video.
With a straw
Best setup, with a white paper below the water bath (to avoid reflection from the heating plate) and OBS was set to manual exposure, which kept the same exposure value throughout the whole recording

## Slide 7: Dataset criteria pH (obtained with NaOH or HCl) and ionic strength (obtained with NaCl) to mimic stomach and intestinal conditions
Acronym | pH | Ionic Strength or IS (mM) | Pepsin
pH 3 IS 0 | 3 | 0 | -
pH 3 IS S | 3 | S | -
pH 3 IS I | 3 | I | -
pH 3 IS S pepsin | 3 | S | yes
pH 7 IS 0 | 7 | 0 | -
pH 7 IS S | 7 | S | -
pH 7 IS I | 7 | I | -
S = Stomach = 98 mM
I = Intestinal = 142 mM

## Slide 8: Data Analysis done by Julia so far
For each recording - run a timelapse script that keeps every 200th frame of the recording
For each timelapse video (around 3 minutes), average grayscale values are calculated over time. Linear regression is performed on the data and plots showing the grayscale trend for each video are generated